## Slide 2
SYNTHETIC RED OXIDE METAL PRIMER
It has good anti-corrosive properties. It contains Zinc-chrome.
Recommended for agricultural, steel structures & other
Machinery, interior and exterior in mildly corrosive marine &
industrial atmosphere.
Manufactured according to I.S. 2074 regulations

## Slide 3
TECHNICAL DATA
Colour : Red Brown
Finish : Matt
Solid Volume : Approx. 33%
Recommended DFT / coat : 20 to 30 microns
Theoretical Covering Capacity : 16.10 m²/l @ 20 microns dft
10.80 m²/l @ 30 microns dft
*Drying Time at 30° C : Surface Dry : 60 minutes
: Hard Dry : 11 hrs.
*Over coating interval at 30° C : Min. : 11 hrs.
: Max. : 3years, provided surface is dry and clean from all contamination.
Shelf life (cool & dry place) : 12 months
Flash Point : Not less than 30° C
Drying and over coating times are related to the film thickness, temperature,
the relative humidity of the air, ventilation & type of “Recoat” paint used.

## Slide 4
DIRECTION FOR USE
SURFACE PREPARATION
Perform blast cleaning. If blast cleaning is impractical, remove loose rust/scale using power tools.
All surfaces must be clean, sound, dry and free of all dirt, dust, wax, oil, grease, chalk and any other contamination that would interfere with new coating adhesion. Bare surfaces must be properly prepared prior to application of this product.
Ideally, the surface should be cleaned by “Solvent 148”.
Surface temperature must be at least 3° C above dew point but not above 50° C.
MIXING
If settling is observed in the drum, loosen the settled material with the help of hand stirrer followed by power driven stirrer for quick homogenous mixing.

## Slide 5
APPLICATION METHOD
BRUSH / ROLLER
Recommended thinner : Synthetic Thinner
Volume of thinner : 00-05 %
AIR SPRAY
Recommended thinner : Synthetic Thinner
Volume of thinner : 05-10 %
Nozzle orifice : 1.5-3.0 mm
Nozzle pressure : 0.3-0.4 MPa (=approx.3-4 atm; 43-57 p.s.i)
AIRLESS SPRAY
Recommended thinner : Synthetic Thinner
Volume of thinner : 00-06 %
Nozzle orifice : 0.37-0.46 mm
Nozzle pressure : 10 to 13.5 MPa (=approx.100 -135 atm; 1400-1890 p.s.i)
STORAGE:- Store in a cool & dry place.Store as per prevailing regulations.
PACKING :- Single Pack: 20 Litres / 04 Litres / 01 Litre

## Slide 6
SAFETY GUIDELINES
This product is for industrial use only by professional applicators and is not intended or suitable for use in or around a household or residential property. Keep away from children and household items. Improper handling and use may be hazardous. Inhalation of solvent vapours or paint mist and contact of liquid paint with skin & eyes, should be avoided.
Forced ventilation should be provided when applying paint in confined spaces or stagnant air. Even when ventilation is provided, skin & eye protection is always recommended while spraying paint. At all times safety precautions must be strictly followed during storage, handling and application. If necessary, kindly refer to our Material Safety Data Sheet for detailed safety measures.
To prevent pollution kindly do not discard tins or pour paint into water courses, use the facilities provided. It is best to allow paints to harden before disposal.

## Slide 7
Contact us
Mr. Kunal Amin,
add:- Packme Indutries,
C-1 , B/2&3, G.I.D.C. Estate
Vithhal Udhyognagar
Gujarat,388121
Telefax:- +91-2692-236173
email us:- info@packmeindustries.com
visit us:- http://www.packmeindustries.com
Thank You